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DATE :17/11/2014

QNA- PR< LSG-Casa Elite E>- 01

To Mr. Uttam Pawar

Project Lakeshore Greens (Sector 3)

Wing Elite (3.07A) — E wing.

Site Inspection Date | 11/11/2014

Description Column C6 between the kitchen & the living room. The concreting

has not been correctly achieved.

Rectification
required

Rectification measures to be taken post discussion with Structural
consultant & Lodha Structure team.
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Honey combing has been observed at many areas.

Rectification
required

Rectification measures to be taken post discussion with Structural
consultant & Lodha Structure team.

The form work of 200 x 400 cut out in the utility has not yet been de
shuttered or has been unknowingly left.

Rectification
required

The formwork to be removed & the opening size to be maintained as
per the dwgs.
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Due to undulations in the slab there is a gap between the vertical
formwork & the slab. 1. There are substantial chances of slurry
leakages at such junctions leading to water seepage pockets in the
building. 2. Also there will be plumb & alignment issues.

Rectification Rectification measures to be taken post discussion with Structural
required consultant & Lodha Structure team.
Issued by :
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Supriya Ambavane < Project Architect>





