Soudafoam PRO
High Performance Gun-Grade Expanding PU Foam
Description:
Soudafoam PRO with CFC-free propellant is a one-component, selfexpanding, ready to use polyurethane foam. It contains CFC-free propellants, which are completely harmless to the ozone layer. It has been tested and approved for soundproofing by "ift Rosenheim".
Applications:
• Installing of window and door frames
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• Sealing of all openings in roof constructions	
• Creation of a soundproof screen
• Mounting and sealing of window and door frames
• Connecting of insulation materials and roof constructions
• Application of a soundproofing layer on motors
• Improving thermal isolation in cooling systems
Properties
Base
Polyurethane
Consistency
Stable foam, thixotropic
Curing system
Moisture cure
Skin formation (20°C/65% R.H.)
Ca 8 minutes
Drying time (20°C/65% R.H.)
Dust free after 20-25 min.
Curing Rate (20°C/65% R.H.)
1h for a 30 mm bead
Yield
1000 ml yields 35-40 L cured foam
Shrink
None
Postexpansion
None
Cellular Structure
Ca 70-80 % closed cells
Specific Gravity
Ca. 25 kg/m³ (extruded, fully cured)
Temperature Resistance
-40°C to +90°C when cured
Colour
Champagne
Fire Class (DIN4102 part2)
B3
Insulation Factor
Ca. 31 mW/m. K
Shear Strength (DIN 53427)
12 N/cm²
Pressure Strength (DIN 53421)
3 N/cm²
Bowing Strength (DIN 53423)
7 N/cm²
Water Absorption
1% Vol. (DIN53429)
Acoustic Rating
RST,W= 58dB
Characteristics:
• Excellent adhesion on most substrates (except Teflon, PE and PP)
• High thermal and acoustical insulation
• Very good filling capacities
• Excellent mounting capacities
• Excellent stability (no shrink or post expansion)
• Very precise application due to the foamgun system resulting in controlled expansion
• Low expansion
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	Champagne
	750ml
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Product Features:
• Soudafoam PRO PU Foam is very easy Installing of window and door frames.
• Soudafoam PRO PU Foam used in Sealing of all openings in roof constructions.
• Soudafoam PRO PU Foam used in Creation of a soundproof screen.

Soudafoam 1K
High Performance One - Component Expanding PU Foam
Description:
Soudafoam 1K is a one-component, selfexpanding, ready to use polyurethane foam with CFC-free propellants, which are completely harmless to the ozone layer.
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• Installation of window and door frames
• Filling of cavities
• Sealing of all openings in roof constructions
• Creation of a soundproof screen
• Mounting and sealing of window and door frames
• Connecting of insulation materials and roof constructions
• Application of soundproofing layers on motors
• Improving thermal insulation in cooling systems
Properties
Base
Polyurethane
Consistency
Stable foam
Curing system
Moisture-cure, thixotropic
Skin formation
Ca. 8 minutes (20°C/65% R.H.)
Drying time
Dust free after 20-25 min. at 20°C
Curing rate
1,5 h for a 30 mm bead (20°C/65% R.H.)
Yield
1000 ml yields 35 L cured foam
Shrink
None
Post expansion
None
Cellular structure
Ca 70-80% closed cells
Specific gravity
Ca 25 g/m³ (extruded, fully cured)
Temperature resistance
-40°C until +90°C when cured
Colour
Champagne
Fire Class (DIN 4102 part2)
B3
Insulation Factor
33 mW/mK
Shear Strength (DIN53427)
17 N/cm²
Pressure Strength (DIN53421)
3 N/cm²
Bowing Strength (DIN53423)
7 N/cm²
Water Absorption (DIN53429)
1% Vol.
Acoustic Rating
RST,W= 58dB
Characteristics:
• Excellent adhesion on most substrates (except Teflon, PE and PP)
• High thermal and acoustical insulation
• Very good filling capacities
• excellent stability (no shrink or post expansion)
• Excellent mounting capacities
	Color:
	Packaging:
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	Champagne
	300 ml and 750 ml aerosol cans
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Product Features:
• Soudafoam 1K PU Foam is a one-component, self expanding, ready-to-use polyurethane foam with 
   CFC-free propellants which are completely harmless to the ozone layer.
• Soudafoam 1K PU Foam used for Installation of window and door frames.
• Soudafoam 1K PU Foam used for Filling of cavities.
• Soudafoam 1K PU Foam used for sealing of all openings in roof constructions.
• Soudafoam 1K PU Foam used for creation of a soundproof screen.
• Soudafoam 1K PU Foam used for Mounting and sealing of window and door frames.
• Soudafoam 1K PU Foam creates soundproofing layers.
• Soudafoam 1K PU Foam used in Installation of air conditioners.
• Soudafoam 1K PU Foam has excellent adhesion on most substrates (except Teflon, PE and PP).
• Soudafoam 1K PU Foam has high thermal and acoustical insulation.
• Soudafoam 1K PU Foam has very good filling capacities.
• Soudafoam 1K PU Foam is available in Champagne color.
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